## Slide 1: EML 4551C SENIOR DESIGN DR. KAMAL AMIN TEAM 4: ALTERATE MATERIAL SELECTION FOR COMPRESSOR CASING IN TURBOCHARGER DESIGN REVIEW PRESENTATION #2 Group Members alexander Mankin HARRISON MCLARTY Ralph Scott Abiodun OLUWALOWO Project sponsor AND FACULTY Adviser Cummins - Roger England DR. PETER KALU 18 MARCH 2014

## Slide 2: Outline
Project Scope
Project Background
Project Objectives
Fall Accomplishments
Design Concepts
Design Analysis
Potential Challenges and Risks
Status of Procurement
Future Work
Final Summary
References
Questions

## Slide 3: Project Scope
Fig.1: View of turbocharger compressor casing.[5]
Cummins has an interest in researching and selecting alternate materials to fabricate compressor casings in their B series turbochargers
This alternate material should ultimately be more cost effective than the current one in use, cast aluminum 356, and still satisfy the design and operational parameters set by Cummins
Estimates of manufacturing costs for this alternate material and verification of burst containment are essential
Harrison McLarty

## Slide 4: Project Background
In industry more cost efficient materials are always being researched
The revenue gained from more cost efficient materials and manufacturing processes present financial advantages for Cummins
Production numbers on compressor casings and turbochargers have the potential to grow allowing the company to meet and exceed the expectations of customers
Finding new materials which could replace cast aluminum 356 presents many beneficial opportunities for Cummins
Harrison McLarty

## Slide 5: Project Objectives
Determine the temperatures, pressures, and stresses experienced by the compressor during operation
Research and compare materials which can operate under these prescribed physical conditions, and are cheaper both as a material and to manufacture
Estimate manufacturing costs with this new material and compare it to cast aluminum 356, which is currently used to fabricate the casings
With the known operational conditions and alternate material known, utilize Finite Element Analysis in conjunction with a CAD model of the casing for analysis
Obtain three prototypes of these casings for testing and experimentation
Harrison McLarty

## Slide 6: Fall 2013 Accomplishments
PEEK(Polyether ether ketone) was selected as the material to be used as the compressor casing after thorough research.
FEA analysis was conducted on a cross section of the casing’s piping to ensure that the material selected would not deform significantly during operation.
A contact at Cummins was found who will obtain prototypes based on our chosen alternate material.
Initial research was begun on carrying out FEA analysis for the burst event.
Harrison McLarty

## Slide 7: Design Concepts: Material for prototype
With the aid of a weighted decision matrix PEEK (unfilled) was found to be the most effective material for fabricating a compressor casing
It possesses the following advantages and superior characteristics:
    Heat resistance at temperatures beyond 230
    Pressure resistance ( resistance to deformation due to pressure)
    Resistance to diesel engine fluids
    Dimensional stability (i.e. low rate of water absorption)
    Excellent balance of yield strength and elongation
Harrison McLarty

## Slide 8: Design Concepts: Need for burst analysis
Fig.2 Example of a burst containment test. [5]
“Burst” occurs when the centrifugal force undergone by impeller wheels, due to their rotational speed, overcome the mechanical strength of the wheel.
Causes of a burst event include:
  Reduction of strength due to high internal stresses associated with high temperatures and speeds
  Fatigue failure due to cyclic loading (i.e. stop and go motion of a city bus)
  Foreign object damage (FOD) (i.e. a rock or piece of rubber impacting a wheel)
Although a rare event, this must be kept in mind when selecting materials for either the compressor or turbine housing due to the safety concern of burst.
Materials with the proper yield strength, % elongation (ductility), and maximum operational temperature must be considered to withstand this event.
Harrison McLarty

## Slide 9: Design Concepts
Injection Molding Cost Analysis
Ralph Scott
Mold Costs
The cost of a mold can vary greatly based on complexity, quality, and size.
Simple, single cavity mold: $2,000-3,000
High production, multi-cavity mold: $60,000-100,000
Addition Injection molding Costs
To gain knowledge on creating a more accurate injection molding cost Analysis, we plan to speak to Dr. Chengying Xu who will hopefully guide us in the right direction to preform proper cost analysis.
Unfortunately Dr. Xu will not be available to meet with us until the week of the 25th of March.

## Slide 10: Design Concepts
Injection Molding Cost Estimation Equations
Ralph Scott
The following are equations that can be used to determine manufacturing cost associated with producing a injection molded part.
1.)
2.)

## Slide 11: Design Concepts
Injection Molding Cost Estimation Equations
Ralph Scott
1.)
The cost drivers of manufacturing injection molded parts are expressed in Equation 1.

## Slide 12: Design Concepts
Injection Molding Cost Estimation Equations
Ralph Scott
2.)
Equation 2 is an expression for the assembled product cost

## Slide 13: Design Concepts
To further validate the safety of the casing, simulation of a burst event was performed
It was performed in Comsol and used the following criteria
Failure Analysis was performed for two different compressor wheel speeds, 90,000 and 120,000 rpm
Due to their design, compressor wheels usually fail by breaking into 2 or 3 pieces
Impact speed was found using the relationship between rotational kinetic energy and kinetic energy of a rigid body
Force was found by using the classic force formula
Alex Mankin

## Slide 14: Burst Containment Analysis 90,000 rpm
Alex Mankin
Fig.4 Cast Aluminum 356 von Mises stress
Fig. 3 PEEK von Mises Stress

## Slide 15: Burst Containment Analysis 90,000 rpm
Alex Mankin
Fig. 5 PEEK Total Displacement
Fig.6 Cast Aluminum 356 Total Displacement

## Slide 16: Burst Containment Analysis 90,000 rpm
Alex Mankin
Fig. 7 PEEK 1st Principle Strain
Fig.8 Cast Aluminum 356 1st Principle Strain

## Slide 17: Burst Containment Analysis 120,000 rpm
Alex Mankin
Fig. 9 PEEK von Mises Stress
Fig.10 Cast Aluminum 356 von Mises stress

## Slide 18: Burst Containment Analysis 120,000 rpm
Alex Mankin
Fig. 11 PEEK Total Displacement
Fig.12 Cast Aluminum 356 Total Displacement

## Slide 19: Burst Containment Analysis 120,000 rpm
Alex Mankin
Fig. 13 PEEK 1st Principle Strain
Fig.14 Cast Aluminum 356 1st Principle Strain

## Slide 20: Burst Containment Analysis Summary
Alex Mankin
The analysis shows that PEEK deforms a higher amount relative to the cast aluminum which is currently used
This deformation occurs the most at the location of impact with smaller deformation occurring in the surrounding material
It also shows that despite this higher amount of deformation the casing still absorbs the burst event adequately and without a catastrophic failure of the material
This result of the burst containment analysis shows that the PEEK material is a valid and safe selection for use as an alternative material
The validity of this analysis could be tested if a real burst test was performed with the PEEK material

## Slide 21: Potential Challenges and Risks
Making sure the assumptions and cost estimations made during the manufacturing cost analysis are accurate, and comparable to real world applications.
Ensuring that our analysis on our 3-D model of the compressor casing, is an accurate representation of the effects the compressor casing would undergo in the field.
Ralph Scott

## Slide 22: Status of procurement
The prototype based on PEEK could not be machined because it could not be procured in a large enough block.
A proprietary powder material was instead used to 3-D print a compressor casing prototype for demonstration purposes only.
Ralph Scott

## Slide 23: Status of procurement
Ralph Scott
Fig.15 3D Printed Compressor Casing

## Slide 24: Future Work Plans
The future plans includes the following:
Calculating and estimating the manufacturing costs using the equations and parameters that was given in the previous slides
Also in order to have accurate cost evaluations some faculty members will be consulted (Dr. Chengying Xu )
Ralph Scott

## Slide 25: Gantt Chart
Ralph Scott

## Slide 26: Conclusions
A burst analysis was completed which showed that PEEK was an adequate replacement for the current material used.
We will continue to refine our manufacturing cost analysis.
We also now have a 3-D printed full scale model of our turbocharger compressor casing for display purposes only
Ralph Scott

## Slide 27: References
1. "Turbo Torque." Turbo Torque. N.p., n.d. Web. 21 Oct. 2013. <http://www.mazdarotary.net/turbo.htm>.
2. "Online Materials Information Resource - MatWeb." Online Materials Information Resource - MatWeb. N.p., n.d. Web. 21 Oct. 2013. <http://www.matweb.com/>.
3. "Plastic Sheet, Plastic Rod, Plastic Tubing - Buy Online." Plastic Sheet, Plastic Rod, Plastic Tubing - Buy Online. N.p., n.d. Web. 21 Oct. 2013. <http://www.professionalplastics.com/>.
4. "VICTREX® PEEK Polymers." High Performance Polyaryletherketones, High Temperature Advanced PEEK Polymer, Thermoplastic. N.p., n.d. Web. 19 Nov. 2013. <http://www.victrex.com/en/products/victrex-peek-polymers/victrex-peek-polymers.php>.
5. "Burst and Containment: Ensuring Turbocharger Safety." Turbobygarrett.com. N.p., n.d. Web. 19 Nov. 2013. <http://www.turbobygarrett.com/turbobygarrett/sites/default/files/Garrett_White_Paper_02_Burst__Containment.pdf>.
6. Fagade, Adekunle A., and David O. Kazmer. "EARLY COST ESTIMATION FOR INJECTION MOLDED PARTS." University of Massachusetts Amherst (n.d.): n. pag. Web.

## Slide 28: Questions